ISO –FILM SPEEDS

Film speed is the measure of a photographic film's sensitivity to light, determined by sensitometry and measured on various numerical scales, the most recent being the ISO system. Relatively insensitive film, with a correspondingly lower speed index requires more exposure to light to produce the same image density as a more sensitive film, and is thus commonly termed a slow film. Highly sensitive films are correspondingly termed fast films.

Applying film speed

Film speed is used in the exposure equations to find the appropriate exposure parameters. Four variables are available to the photographer to obtain the desired effect: lighting, film speed, f-number (aperture size), and shutter speed (exposure time).

USE PARTICUALR FILM SPEEDS ACCORDING TO THE TIME OF DAY…REMEMBER THIS ALLMUST WORK IN COMBINATION WITH YOUR APERTURE SIZE AND SHUTTER SPEED

Common Film Speeds

DAY LIGHT				AFTERNOON				NIGHT

100					400					800

125					500					1000

160					640					1250

200										1600

250										2000

320